## Slide 1
Preparation and Characterization of Lipid Coated Silica Nanoparticles
Raz Jelinek lab
The Department of Chemistry ​Ilse Katz Institute for Nanoscale Science & Technology
Ben-Gurion University of the Negev
Presented by: Daniel N. Bloch

## Slide 2
Ethanol water Ammonium hydroxide
TEOS (silicon source)
Stir for two hours
Dry under vacuum
Dissolve in lipids, vortex for half an hour
Preparation of Coated Silica Nanoparticles
Rinse several times
Coated Silica Nano Particles

## Slide 3: Lipid Compositions
DOPC
POPC
DPPC
Sample | Composition | mole ratio
1 | DOPC/POPC | 100/0
2 | DOPC/POPC | 70/30
3 | DOPC/POPC | 50/50
4 | DOPC/POPC | 30/70
5 | DOPC/POPC | 0/100
Sample | Composition | mole ratio
1 | DOPC/DPPC | 100/0
2 | DOPC/DPPC | 70/30
3 | DOPC/DPPC | 50/50
4 | DOPC/DPPC | 30/70
5 | DOPC/DPPC | 0/100

## Slide 4
Chart: zeta potential
| si | 100/0 | 70/30 | 50/50 | 30/70 | 0/100
DOPC/POPC | -17.52 | -6.026 | -4.662 | -3.972 | -6.964 | -4.026
DOPC/DPPC | -17.52 | -3.662 | -6.964 | -6.114 | -4.354 | -4.308
Proof for Coating- Zeta Potential
Determining the vesicles surface potential by Zeta Potential

## Slide 5
So3-
Proof for Coating by Rhodamin Emission
 | % Of the lipid in the coating DOPC/POPC composition | % Of the lipid in the coating DOPC/DPPC composition
100/0 | 61 | 64
70/30 | 62 | 48
50/50 | 53 | 71
30/70 | 38 | 58
0/100 | 77 | 26
N_Rhodamin_PE dye
Located on bilayer membrane surface
The amount of lipids in the coating is determined by Rhodamin emission
Before cleaning free lipids in the solution
after cleaning free lipids in the solution

## Slide 6: Fluorescence Anisotropy
Masurement of the bilayer fluidity through anisotropy of TMA-DPH and DPH probes
0
Fluid membrane
0.4
Rigid membrane
TMA-DPH
DPH
DPH
TMA-DPH

## Slide 7
Fluorescence Anisotropy Results
Chart: 
| 100/0 | 70/30 | 50/50 | 30/70 | 0/100
day 1 | 0.2393 | 0.25104 | 0.24659 | 0.2334 | 0.26628
day 2 | 0.23687 | 0.22847 | 0.2328 | 0.23832 | 0.26926
day 3 | 0.23236 | 0.23966 | 0.23027 | 0.23027 | 0.27637
day 5 | 0.22314 | 0.2324 | 0.24507 | 0.22585 | 0.26598
day 7 | 0.23996 | 0.23752 | 0.23553 | 0.23055 | 0.27086
TMA-DPH DOPC/POPC

## Slide 8
DPH DOPC/POPC
Chart: 
| 100/0 | 70/30 | 50/50 | 30/70 | 0/100
day 1 | 0.11205 | 0.11772 | 0.13845 | 0.15968 | 0.24666
day 2 | 0.11228 | 0.12808 | 0.16856 | 0.13248 | 0.26501
day 3 | 0.11388 | 0.11984 | 0.15779 | 0.12824 | 0.25311
day 5 | 0.11363 | 0.13498 | 0.18545 | 0.13505 | 0.27949
day 7 | 0.1165 | 0.1238 | 0.15431 | 0.13578 | 0.24838
Fluorescence Anisotropy Results

## Slide 9
TMA-DPH DOPC/DPPC
Chart: 
| 100/0 | 70/30 | 50/50 | 30/70 | 0/100
day 1 | 0.22118 | 0.22743 | 0.23006 | 0.23521 | 0.32626
day 2 | 0.22637 | 0.22082 | 0.2271 | 0.22281 | 0.32738
day 3 | 0.23994 | 0.23149 | 0.24705 | 0.21901 | 0.33131
day 5 | 0.23816 | 0.22916 | 0.23781 | 0.21637 | 0.34711
day 7 | 0.22838 | 0.22791 | 0.22589 | 0.2275 | 0.3174
Fluorescence Anisotropy Results

## Slide 10
DPH DOPC/DPPC
Chart: 
| 100/0 | 70/30 | 50/50 | 30/70 | 0/100
day 1 | 0.11694 | 0.1276 | 0.12342 | 0.11227 | 0.34455
day 2 | 0.11338 | 0.1261 | 0.12659 | 0.11662 | 0.35041
day 3 | 0.10675 | 0.12491 | 0.10905 | 0.11345 | 0.35438
day 5 | 0.1027 | 0.13077 | 0.12064 | 0.12095 | 0.34762
day 7 | 0.11089 | 0.12342 | 0.11815 | 0.11463 | 0.34625
Fluorescence Anisotropy Results

## Slide 11
Characterization of coated nanoparticles Dimensions
AFM- DOPC/POPC Composition
Height Profile

## Slide 12
Silica Nano Particles Coating Thickness
Contact with the lipid layer:
The force increases
The distance does not change
Penetration of the lipid layer:
The force decreases
The distance decreases
Contact with the silica nanoparticle:
The force increases
The distance does not change

## Slide 13
Silica Nano Particles Coating Thickness
DOPC/POPC composition
Force-Distance curves on several particles
5nm

## Slide 14
DOPC/DPPC composition
Height Profile
Characterization of coated nanoparticles Dimensions

## Slide 15
Silica Nano Particles Coating Thickness
DOPC/DPPC composition
Magnified view
4.4nm
Force-Distance curves on several particles